# Polymer-regulated BiOCl: Structural and defect evolution enabling in situ Bi formation and multifunctional catalysis

Youhai Huang a, Jianyun Bai a, Ruize Yan b, Wenjun Zhang a, Sifan Zhang a, Yanjun Zhang a, Meng Chen a*

a State Key Laboratory of Coatings for Advanced Equipment, College of Smart Materials and Future Energy, Fudan University. 220 Handan Road, Shanghai 200433, P. R. China

b Shanghai Starriver Bilingual School, 2588 Jindu Road, Shanghai, P. R. China

*Corresponding author: Meng Chen

E-mail address: chenmeng@fudan.edu.cn (Meng Chen)

Figures: 5.

Tables: 3.

Contents:

Fig.S1. (a) XRD patterns of samples prepared in the absence of KCl, with and without PSSMA; (b) XRD pattern of BiOCl–PSSMA after solvothermal treatment.

Fig.S2. XRD patterns of BiOCl synthesized after 4 h solvothermal reaction with different PSSMA contents: 0.4, 0.6, and 0.8 g.

Fig.S3. XRD patterns of BiOCl synthesized after 10 h solvothermal reaction with varying PSSMA contents.

Fig.S4. Photographs of precursor solutions in the ethylene glycol–water system before solvothermal treatment: (a) KCl; (b) Bi(NO₃)₃·5H₂O; (c) KCl + Bi(NO₃)₃·5H₂O; (d) KCl + Bi(NO₃)₃·5H₂O + PSSMA; (e) KCl + PSSMA; (f) Bi(NO₃)₃·5H₂O + PSSMA

Fig.S5. Calibration curve for H₂O₂ determined by the potassium iodide spectrophotometric method: (a) UV–vis absorption spectra of H₂O₂ at different concentrations; (b) corresponding calibration curve.

Fig.S6.

Table S1. Mass fractions of Bi and BiOCl estimated by the semi-quantitative RIR method.

Table S2. Comparison of the photocatalytic degradation performance of BiOCl-PSSMA with those of other reported catalytic materials.

Table S3. Comparison of the ultrasound-driven H₂O₂ production performance of BiOCl-PSSMA/Bi with those of other reported catalytic materials.

Fig.S 1. (a) XRD patterns of samples prepared in the absence of KCl, with and without PSSMA; (b) XRD pattern of BiOCl–PSSMA after solvothermal treatment.

Fig.S2. XRD patterns of BiOCl synthesized after 4 h solvothermal reaction with different PSSMA contents: 0.4, 0.6, and 0.8 g.

Fig.S3. XRD patterns of BiOCl synthesized after 10 h solvothermal reaction with varying PSSMA contents.

Fig.S4. Photographs of precursor solutions in the ethylene glycol–water system before solvothermal treatment: (a) KCl; (b) Bi(NO₃)₃·5H₂O; (c) KCl + Bi(NO₃)₃·5H₂O; (d) KCl + Bi(NO₃)₃·5H₂O + PSSMA; (e) KCl + PSSMA; (f) Bi(NO₃)₃·5H₂O + PSSMA.

Fig.S5. Calibration curve for H₂O₂ determined by the potassium iodide spectrophotometric method: (a) UV–vis absorption spectra of H₂O₂ at different concentrations; (b) corresponding calibration curve.

Fig.S 6. XRD patterns of BiOCl-PSSMA/Bi before (black) and after (red) a single H₂O₂ production cycle.

ωa=IaIa+(Ib*RIRaRIRb)

ωb=IbIb+(Ia*RIRbRIRa)=1-ωa

Table S1. Mass fractions of Bi and BiOCl estimated by the semi-quantitative RIR method.

| Sample | ωBi (%) | ωBiOCl (%) |
| --- | --- | --- |
| BiOCl-PSSMA/Bi (10 h) | 22.5 | 77.5 |
| BiOCl-PSSMA/Bi (24 h) | 23.5 | 76.5 |

Table S2. Comparison of the photocatalytic degradation performance of BiOCl-PSSMA with those of other reported catalytic materials.

| Material |  | Loading /mg |  |  |  | Concentration （mg/L） |  | Pollutant |  | Light | k/min-1 |  | Ref. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BiOBr/BiOCl/AgBr |  | 10 |  | 20 mg/L |  |  |  | RhB |  | 210 W Xe λ＞420 nm | 0.118 |  | [1] |  |
| Bi2O2CO3/Bi/BiOCl |  | 60 |  | 20 |  | RhB |  | 300 W Xe λ＞420 nm |  |  | 0.211 |  | [2] |  |
| graphene oxide/MIL-88A(Fe) |  | 20 |  | 10 |  | RhB |  | 500 W Xe 420 nm< λ < 760 nm |  |  | 0.0645 |  | [3] |  |
| BiOCl-PSSMA |  | 10 |  | 30 |  | RhB |  | 300 W Xe λ＞420 nm |  |  | 0.2609 |  | This Work |  |
| TiO2@rGo |  | 25 |  | 20 |  | Rh6G |  | 300 W Hg λ > 400 nm |  |  | 0.0497 |  | [4] |  |
| ZnO-Br |  | 50 |  | 4.8 |  | Rh6G |  | 125 W Hg λ < 400 nm |  |  | 0.0102 |  | [5] |  |
| Au-ZnO |  | 10 |  | 4.8 |  | Rh6G |  | 300 W Xe |  |  | 0.1780 |  | [6] |  |
| BiOCl-PSSMA |  | 10 |  | 20 |  | Rh6G |  | 300 W Xe λ＞420 nm |  |  | 0.1729 |  | This Work |  |
| SnO2/Zn2–SnO4 |  | 100 |  | 10 |  | MG |  | 15W UV lamp |  |  | 0.029 |  | [7] |  |
| ZnO/GO |  | 100 |  | 10 |  | MG |  | 100 W UVA λ = 395 nm |  |  | 0.1214 |  | [8] |  |
| YMnO3-doped TiO2 |  | 10 |  | 2.2 |  | MG |  | 125W HG λ = 454 nm |  |  | 0.0228 |  | [9] |  |
| BiOCl-PSSMA |  | 10 |  | 40 |  | MG |  | 300 W Xe λ＞420 nm |  |  | 0.1729 |  | This Work |  |
| AC-DTE@BiOCl |  | 20 |  | 10 |  | TCH |  | 300 W Xe λ＞420 nm |  |  | 0.0184 |  | [10] |  |
| Ta-Bi24O31Cl10/BiOCl |  | 10 |  | 10 |  | TCH |  | 300 W Xe λ＞420 nm |  |  | 0.0158 |  | [11] |  |
| BiOCl0.2Br0.8 |  | 20 |  | 50 |  | TCH |  | 300 W Xe λ＞420 nm |  |  | 0.0219 |  | [12] |  |
| BiOCl-PSSMA |  | 20 |  | 20 |  | TCH |  | 300 W Xe λ＞420 nm |  |  | 0.0935 |  | This Work |  |

Table S3. Comparison of the ultrasound-driven H₂O₂ production performance of BiOCl-PSSMA/Bi with those of other reported catalytic materials.

| Material | Ultrasonic Power | H2O2 Production | Ref. |
| --- | --- | --- | --- |
| BiOCl-rich OVs | 150 W, 53 kHz | 560 µmol·g-1·h-1 | [13] |
| Bi0.5Na0.5TiO3 | 150 W, 53 kHz | 469 µmol·g-1·h-1 | [14] |
| g-C3N4 | 150 W, 53 kHz | 680 µmol·g-1·h-1 | [15] |
| RbBiNb2O7/ poly(tetrafluoroethylene) | 240 W, 68 kHz | 219.23 µmol·g-1·h-1 | [16] |
| BiOCl-PSSMA/Bi | 540 W, 40 kHz | 760 µmol·g-1·h-1 | This Work |

# References

[1]	X.-H. Zheng, W. Chen, M.-N. Xu, C. Cai, F. Yang, Photocatalytic properties of BiOBr/BiOCl/AgBr ternary photocatalysts for degradation of RhB dye, J. Nanoparticle Res. Interdiscip. Forum Nanoscale Sci. Technol. 25 (2023) 96. https://doi.org/10.1007/s11051-023-05748-9.

[2]	Y. Qi, J.-J. Zhang, W.-Y. Li, X. Zhang, T. Guo, C. Zhang, Facile construction of SPR effect assisted Bi2O2CO3/Bi/BiOCl Z-scheme heterostructure for robust photocatalytic decontamination of RhB, Appl. Surf. Sci. 669 (2024) 160543. https://doi.org/10.1016/j.apsusc.2024.160543.

[3]	N. Liu, W.-Y. Huang, X.-D. Zhang, L. Tang, L. Wang, Y. Wang, M. Wu, Ultrathin graphene oxide encapsulated in uniform MIL-88A(Fe) for enhanced visible light-driven photodegradation of RhB, Appl. Catal., B 221 (2018) 119–128. https://doi.org/10.1016/j.apcatb.2017.09.020.

[4]	S.-Y. Pu, R.-X. Zhu, H. Ma, D. Deng, X. Pei, F. Qi, W. Chu, Facile in-situ design strategy to disperse TiO2 nanoparticles on graphene for the enhanced photocatalytic degradation of Rhodamine 6G, Appl. Catal., B 218 (2017) 208–219. https://doi.org/10.1016/j.apcatb.2017.06.039.

[5]	S.B. Satpal, A.A. Athawale, Insights into the effect of halide enriched ZnO synthesized using tetrabutylammonium halides toward photocatalytic degradation of Rhodamine 6G, Environ. Prog. Sustainable Energy 40 (2021) e13709. https://doi.org/10.1002/ep.13709.

[6]	Y.-F. Cheng, W.-L. Jiao, Q.-Q. Li, Y. Zhang, S. Li, D. Li, R. Che, Two hybrid Au-ZnO aggregates with different hierarchical structures: A comparable study in photocatalysis, J. Colloid Interface Sci. 509 (2018) 58–67. https://doi.org/10.1016/j.jcis.2017.08.077.

[7]	P.V.M. Muguirrima, R.T. Doumbi, M.A.M. Castro, C.L.O.D. Rocha, A.M. Mendes, T.B.O. Nunes, M.R.D. Bomio, F.V. Motta, M.A. Correa, C.A. Paskocimas, A.E. Martinelli, Sol–Gel synthesis of SnO2/Zn2–SnO4 heterostructure for the photocatalytic degradation of Malachite Green, ACS Omega 11 (2026) 15494–15507. https://doi.org/10.1021/acsomega.5c13476.

[8]	S. Stanković, M. Radovanović, S. Đorđievski, V. Nedelkovski, B. Markoli, S. Milić, M. Antonijević, Sustainable production and characterization of ZnO–GO nanocomposites from waste Zn–C batteries for photocatalytic degradation of Malachite Green, Metals 16 (2026) 71. https://doi.org/10.3390/met16010071.

[9]	Y. Yulizar, I. Abdullah, R.M. Surya, N.L. Alifa, Green synthesis of novel YMnO3-doped TiO2 for enhanced visible-light-driven photocatalytic degradation of malachite green, J. Environ. Manage. 342 (2023) 118139. https://doi.org/10.1016/j.jenvman.2023.118139.

[10]	C. Fei, Z.-C. Dong, H.-Q. Zhou, T. Xu, K. Tang, Y. Fan, C. Chen, D. Ju, Z. Zhu, H. Ma, R. Mao, Fabrication of high-performance 3D Biochar-Silica@BiOCl composites for photocatalytic degradation of tetracycline hydrochloride, J. Colloid Interface Sci. 697 (2025) 137920. https://doi.org/10.1016/j.jcis.2025.137920.

[11]	M. Yang, Z.-Z. Shi, S.-D. Sun, B. Yang, J. Cui, J. Li, D. Yun, N. Lei, Structure-phase transformation of bismuth oxide to BiOCl/Bi24O31Cl10 shoulder-by-shoulder heterojunctions for efficient photocatalytic removal of antibiotic, J. Environ. Sci. 149 (2025) 149–163. https://doi.org/10.1016/j.jes.2023.09.019.

[12]	Y. Wang, S.-Q. Zhang, Y.-X. Yan, H. Ren, J. Chen, L. Liu, X. Wu, Multi-anions-coupled electronic states in Cl−-doped BiOBr induce highly efficient decomposition of tetracycline hydrochlorid, Mater. Res. Bull. 158 (2023) 112045. https://doi.org/10.1016/j.materresbull.2022.112045.

[13]	D.-K. Shao, L. Zhang, S.-M. Sun, W. Wang, Oxygen reduction reaction for generating H2O2 through a piezo-catalytic process over bismuth oxychloride, ChemSusChem 11 (2018) 527–531. https://doi.org/10.1002/cssc.201702405.

[14]	Y. Zhang, Y.-Z. Lin, R.-F. Li, Z. Chen, D. Zeng, S. Chen, W. Wang, L. Zhang, W. Wang, H. Nie, G. Wang, Enhanced piezo-catalytic H2O2 production over Bi0.5Na0.5TiO3 via piezoelectricity enhancement and surface engineering, Chem. Eng. J. 465 (2023) 143043. https://doi.org/10.1016/j.cej.2023.143043.

[15]	K.-F. Wang, D.-K. Shao, L. Zhang, Y. Zhou, H. Wang, W. Wang, Efficient piezo-catalytic hydrogen peroxide production from water and oxygen over graphitic carbon nitride, J. Mater. Chem.A 7 (2019) 20383–20389. https://doi.org/10.1039/C9TA06251C.

[16]	Y.-L. Ma, B. Wang, Y.-Z. Zhong, Z. Gao, H. Song, Y. Zeng, X. Wang, F. Huang, M.-R. Li, M. Wang, Bifunctional RbBiNb2O7/poly(tetrafluoroethylene) for high-efficiency piezocatalytic hydrogen and hydrogen peroxide production from pure water, Chem. Eng. J. 446 (2022) 136958. https://doi.org/10.1016/j.cej.2022.136958.